## Slide 1: Silicon Research for the Einstein Telescope
Ronny Nawrodt
G. Hofmann, D. Heinert, C. Schwarz, J. Komma, P. Pastrik, S. Kroker (FSU)
I. W. Martin, L. E. Wittrock, E. Wisniewski-Barker, A. Cumming, K. Haughian, P. Murray, G. D. Hammond, M. Abernathy, K. Craig, A. A. v. Veggel, N. Beveridge, J. Hough, S. Rowan (IGR)
S. Reid (UWS)
4th general ET meeting
Hannover 04.12.2012

## Slide 2: Overview
Introduction (Why cryogenics and silicon?)
Properties we know
Unknown parameters and future work
Summary

## Slide 3: Increased sensitivity of ET
aim: 10x increased sensitivity between generations
x 10
x 10

## Slide 4: Increased sensitivity of ET
[S. Hild et al., CQG 27 (2010), ET-0135B-10, ET Design Study]

## Slide 5: Cryogenic Mirrors / Suspensions
Brownian thermal noise (mirror, suspension) ~ T
-> low temperatures AND low mechanical loss needed
amorphous materials
(e.g. fused silica):
loss peak at cryogenic
temperatures
crystalline materials:
low mechanical loss at
low temperatures

## Slide 6: Cryogenic Mirrors / Suspensions
Why Silicon as test mass material?
  large beam diameters needed to reduce thermal noise  large substrates needed (up to 450-500 mm)
  only a few crystalline materials available with such a size  currently probably JUST silicon
intensive studies of parameters needed
  see talks/contributions at this meeting

## Slide 7: Silicon Crystal Production
Matthias Renner
Czochralski method (CZ)
Float Zone method (FZ)
other methods available but less common

## Slide 8: Silicon Impurities vs. Growing Method
Czochralski method:
  large diameters possible (up to 450mm already demonstrated)
  silica crucible introduces impurities (mainly oxygen)
  large interest from semiconductor industry as oxygen impurities are electronically not active
Float Zone method:
  smaller samples (up to 200mm in production)
  limited general interest (e.g. selected optical applications and high power devices)

## Slide 9: Silicon – Mechanical Loss
very high Q-factor at low temperatures
dips in curve related to impurities
current high quality material shows high Q-factor without dips

## Slide 10: Silicon – Mechanical Loss
detailed study of impurities: oxygen in silicon
mechanical loss peak at around 120K  important for LIGO3?
no influence at estimated operating temperature of ET (10-20 K)
both CZ and FZ usable for ET from mechanical loss point of view
details: poster by G. Hofmann et al.

## Slide 11: Silicon – Mechanical Loss
strong contribution from surfaces and their roughness
„smooth“
„rough“
example: Si flexures

## Slide 12: Silicon – Surface Loss
mechanical loss (surface loss)
origin of occuring peak so far unclear:
- lower underground loss might reveal a hidden loss peak
- loss peak is accociated with the etching-process -> surface effect? radiation damage?

## Slide 13: Silicon – Surface Treatments
surface treatments
plasma treatment
(etching, termination)
selective wet chemical
etching

## Slide 14: Silicon – Surface Treatments
Why is a surface treatment and its understanding important?
  reduction of mechanical loss of bulk
  strong influence in suspension design (small structures)
  see talk by:
  G. Hammond (suspensions), K. Haughian (silicate bonding)
  special treatments to realize grating structures
  see talk by S. Kroker

## Slide 15: Silicon as an optical material
silicon not transparent at 1064nm (about 10cm-1)  change of wavelength needed towards longer wavelength
telecom wavelength around 1550nm well suited as lasers/optics exist
several optical parameters need to be studied (e.g. n(T), dn/dT, optical absorption, etc.)

## Slide 16: Silicon – Optical Absorption
energy gap absorption
Ephoton > Egap
additionally: phonon emission/absorption for conservation of momentum
free carrier absorption
no minimum energy (always present!)
carrier density strongly temperature dependent
VB
CB
VB
CB

## Slide 17: Silicon – Optical Absorption
electronic contribution (gap absorption)

## Slide 18: Silicon – Optical Absorption
free carrier contribution
but: initial measurements at Stanford showed 35 ppm/cm or ~200 ppm/cm at Hannover at room temperature
more news: see talk by J. Degallaix (LMA)
fibre amplifier demaged

## Slide 19: Silicon
Does high absorption rule out silicon?
input mirror of arm cavities are the only transmissive silicon mirrors
moderate laser power
due to high thermal conductivity and low thermo-refractive index thermal lensing is reduced
not hunting for 1ppm/cm
heat extraction through suspension will set limit

## Slide 20: Silicon – thermo-refractive index
 very low dn/dT at low temperatures
 limitation for all phase change based absorption techniques (deflection, PCI, etc.)

## Slide 21: Silicon – Thermal Properties
thermal properties (overview)
[Touloukian 1972]
well studied property
strongly size dependent
also: dependent on surface quality (roughness)

## Slide 22: Silicon – some future work
further studies of optical properties of silicon towards real sized mirrors:
  homogeneity of optical properties
  stress induced birefringence
  „natural“ birefringence (e.g. from crystal pulling technique)
content of the joint Aspera proposal

## Slide 23: Link to Kagra Community
operation of cryogenic detector -> technology transfer (ELiTES project)
exchange of knowledge on mechanical loss (Sapphire, Silicon), suspension design and lots of technological issues
currently: visits ongoing (Japan -> Europe)
status of the work: see poster by R. Douglas and talk by Y. Sakakibara

## Slide 24: Summary
silicon as mechanical and optical material for future GW detectors
promising parameters
ongoing research:
  breaking strength
  optical absorption -> Which level can be tolerated? -> suspensions
  homogeneity of optical parameters
  thermal conductivity vs. surface treatment
  mechanical loss vs. surface treatment